Project Name

# Description of the fabrication project

Brief description of your project in few lines, with fabrication keypoints if there are …

Here is an example of process flow that show you some fabrication steps and the way you can describe them. Each step number corresponds to those of the runcard. For your drawings, try to respect aspect-ratios as much as possible.

| Technologies used !! remove non-used !! |  |  |  |
| --- | --- | --- | --- |
| Mask fabrication, LPCVD, PECVD, sputtering, evaporation, positive resist, negative resist, SU-8, Polyimide, Lift-off, Dry etching, Wet etching, E-beam lithography, FIB, Electro-Plating, Wafer Bonding, CMP, Dicing, SEM |  |  |  |
| Ebeam litho data - Photolitho masks - Laser direct write data |  |  |  |
| #### Mask # | Critical #### Dimension | #### Critical Alignment | #### Remarks |
| #### 1 | #### 2um | #### First Mask | #### Oxide structuration |
| 2 | 20 um | 2um | Metal structuration |
| 3 | 20um | 10 um | KOH mask |
| Substrate Type and size |  |  |  |
| Silicon <100>, Ø100mm, 525um thick, Single Side polished, Prime, p type, 0.1-0.5 Ohm.cm |  |  |  |

# Interconnections and packaging of final device

Thinning/grinding/polishing of the samples is required at some stage of the process.

Dicing of the samples is required at some stage of the process.

Wire-bonding of dies, with glob-top protection, is required at the end of the process.

# Step-by-step process outline

| Step | Process description | Cross-section after process |
| --- | --- | --- |
| 01 | Handle wafer oxidation Machine: CentroTherm WetOx Thick: 1-5 um |  |
| 02 | Coating |  |
| 03 | Developement |  |
| 04 | Etching SF6 |  |
| 05 | Surface treatment Machine: Z06 – Cleaner + Surface activation |  |
| 06 | Wafer Bonding Machine: Z06 – EVG 501bonding line + Inspection of bonding |  |
| 07 | ## Anealing 800°C Centrotherm four 3,4 |  |
| 08/09 | Device layer grinding Machine: Z11 DISCO Grinder Thickness: 1-10 um range + Eventual Si etching |  |
| 10 | Device layer CMP Machine: Z18 CMP |  |