Projects at the EPFL Center of MicroNanoTechnology

| ## III-nitride based blue vcsels |  |  |
| --- | --- | --- |
| G. Cosendey, A. Castiglia, G. Rossbach, J.-F. Carlin, N. Grandjean (SB-IPHYS-LASPE) Laboratory of Advanced Semiconductors for Photonics and Electronics, EPFL |  |  |
| # Project objective: Highly-reflective dielectric-based distributed Bragg reflectors (DBRs) have been developed (Fig. 1) to serve as top mirror in blue vertical cavity surface emitting lasers (VCSELs). A schematic drawing and an SEM cross-section view of such a device are depicted in Fig. 2 and Fig. 3, respectively. Electroluminescence (EL) spectra measured below and above threshold on a blue VCSEL are shown in Fig. 4. |  |  |
| Figure 1: Reflection R and transmission T of a 7-pair SiO2/TiO2 DBR. |  | Figure 2: Schematic drawing of a monolithic nitride-based VCSEL. |
| Figure 3: SEM cross-section view of a processed VCSEL. |  | Figure 4: VCSEL EL spectra below and at lasing threshold. |
| Techniques employed: E-beam evaporator (LAB600) for dielectric DBR deposition. |  |  |
| Publications: |  |  |
| [1] | G. Cosendey, A. Castiglia, G. Rossbach, J.-F. Carlin, and N. Grandjean, Blue monolithic AlInN-based vertical cavity surface emitting laser diode on free-standing GaN substrate, Appl. Phys. Lett. 101, 151113 (2012). |  |
| [2] | G. Cosendey, J.-F. Carlin, N. A. K. Kaufmann, R. Butté, and N. Grandjean, Strain compensation in AlInN/GaN multilayers on GaN substrates: Application to the realization of defect-free Bragg reflectors, Appl. Phys. Lett. 98, 181111 (2011). |  |
| Funding: NCCR QP, FNS, CTI/KTI. |  |  |